# Physics - Matters

## Solid

### Structures:

Crystalline solids

Atoms and molecules are arranged in a regular manner

Crystal consists of a basic structure that repeated many times to form the whole crystal

Unit cell

Example: Ionic salt, metallic lattice, graphite

Amorphous solids

Atoms arranged in no order

Have no long range order which the crystalline solids have

### Extension & length:

When an external force is applied to a wire, it extended / has deformation

When the force vanished, the wire return to the original state

Elastic

The tension force F applied to the wire is proportional to its extension (

Tension required to produce the extension ( ( Cross-sectional area A of the wire

Under a particular tension, extension ( ( Length of the wire (

,	the proportionality constant E is called Young modulus

A measure of stiffness

### Stress & strain:

Stress: Tension per unit cross-sectional area

Tensile stress: , unit: Pa

Strain: Extension per unit length of wire, i.e. fractional elongation

Stress ( Strain:	  (   (

Hooke’s Law

Stress-strain curve:

 ( u only if stress is small

Material deforms elastically and obeys Hooke’s law

Btw proportional limit P and elastic limit L, stress-strain relation is not linear but still in elastic deformation

Usually, smaller stress causes a larger strain than usual

The material is less stiff

Exceeds elastic limit, the material undergoes plastic deformation

When stress removed, the material does not return to the original state

Permanent deformation

Before Y, the material return to O' instead of O when stress removed

Beyond yield point Y,  The material stays where it is when the stress is removed

Thinning

Breaking stress M is the maximum stress a material can withstand

Tensile strength

Compression: Negative stress

Hooke’s law holds for small compression

For large compression, the material is stiffer than tension

### Mechanical Properties:

Stiffness: Resistance to deformation under the application of forces

Stiff material has a higher Young modulus than a soft material

Strength: Ability to withstand forces without breaking

Strong material has a higher breaking stress than a weak material

Ductility: A ductile material elongates appreciably before it breaks

Displays a large among of plastic deformation

Brittleness: A brittle material breaks soon after the yield point is reached

Can withstand only small deformations

Stiff but not strong

### Energy:

Material at its natural state has the lowest energy

When material is stretched / compressed, it possess a higher PE U

Increased PE U = Work done W to deform the object

Work done:

A solid of unit length and unit cross-sectional area,

PE stored per unit volume

A solid of length ( & cross-sectional area A, total PE stored:

;

Elastic deformation: The PE absorbed is released completely when stress removed

Plastic deformation: The PE absorbed is partially released when stress removed, but partially used to deform the object to other shape

### Elastic Hysteresis:

Stress-strain behavior of rubber is different from other crystalline solid:

Has a large range of elasticity

Does not obey Hooke’s law within elastic limit

Soft at small strains but stiff at large strains

In microscopic view, rubber comprising molecular chains coil up and tangle with one another

Small stress ( Straighten the chains

Further strain after straightened out ( Much greater stress required

Stress removed ( Coil up again

In stress-strain curve, stretching & relaxing behavior differs

The curves for stretching & relaxing does not coincide

Elastic hysteresis

The area bounded by hysteresis loop is the energy absorbed by rubber

Energy absorbed as heat (internal fiction of molecular chains)

### Intermolecular forces & potential:

In a solid, atoms are held together by inter-atomic forces

When atoms are too close, the inter-penetration of electron shells produce a repulsive force

When atoms are close, bonding formed by inter-atomic electrostatic attraction

When atoms are too far apart, the inter-atomic forces are negligible

Distance btw neighboring atoms = r

The PE U btw two atoms depends on r

U is minimum at the equilibrium separation r0

Not squeezed nor extended

Umin is the bond energy

Force:

F  0: Net repulsion, r  r0

F  0: Net attraction, r  r0

Near r0, the F-r graph is approx. linear

For small stress, Force ( Extension or compression

### Interpretation of Young’s modulus:

Consider an analog model of solid: Particles linked by springs in a cubic array

Cross-sectional area = A

Length of a side = (

Equilibrium separation btw atoms = x

Force constant of each spring = k

When the cubic array is stretched for an extension (,

No. of atoms stretched = No. of atoms on cross-sectional surface =

Extension on each spring = x

Total stretching force required:

Stress:

Strain:

Young’s modulus:

### Thermal expansion:

The U-r graph is asymmetric about r0

Steeper for compression and flatter for stretching

Let U = –U0 when r = r0

At 0K, atoms in a material are stationary at r0

KE = 0; PE = –U0

Above 0K, there is some thermal energy in the material

KE  0; Atoms oscillate about the equilibrium position r0

Some molecular KE will turn to molecular PE during oscillation

Conservation of energy

U rose, the atoms oscillating btw r = a & r = b

Mean interatomic separation = m

Raising temperature, U rose as more thermal energy in the material

The atoms oscillating btw r = a' & r = b'

Mean interatomic separation = m'

Since m'  m, the average distance btw atoms increased, the solid expanded

## Fluids in Motion

### Flow of fluid:

Turbulent flow: The fluid flows in irregular paths

Eddies may form

Depriving energy from the system

Streamlined flow: The fluid flows in layers without fluctuations or turbulence

Flow velocity at a fixed pt is constant and independent of time

Turbulence occur or not depends on the flow velocity and shape of the objects

If an fluid flowing in a tube,

Volume of fluid in the tube is fixed

In same time interval t, Mass of fluid flowing into the tube = Mass flowing out of the tube

1A1v1t = 2A2v2t  (  1A1v1 = 2A2v2

Equation of continuity: Av = Constant

If the fluid is incompressible, A1v1 = A2v2

Speed of flow at smaller cross-sectional area is higher

### Bernoulli’s Principle:

Ideal fluids:

Non-viscous: No mechanical energy can be converted into internal energy

Incompressible: Density  of the fluid is constant

Fluid is moving with streamlined flow / steady flow: No turbulence

Irrotational flow: Fluid has tranlational motion only

When a ideal fluid is flowing in a tube:

In time interval t, mass of fluid transferred in:
		m = A1v1t

Mass of fluid transferred out:	 m = A2v2t

The fluid flows up as there is a pressure difference

Net force pushes the fluid up = P1A1 – P2A2
( Total work done: P1A1v1t – P2A2v2t =

Ek 

Ep = mgh2 – mgh1 = mg(h2 – h1)

Total work done = Ek + Ep
( 
(

Bernoulli’s equation: = Constant

As the speed of fluid flow increases, fluid pressure reduces

If there is a flow speed difference round an object, pressure difference would be created

Pushing the object towards the side w/lower pressure (higher speed)

### Application of Bernoulli’s principle:

Airfoil

Upper side has a more curved surface than lower side

The upper side increases the speed of air flow

The pressure difference set up to create a net lifting force

Spinning golf ball

When a ball spin through the air, air is dragged by the spinning motion

The spinning cause an increase of air flow on one side and decrease on other side due to the viscous force

Unequal pressure set up on opposite sides

Curve in flight (Magnus effect)

Yacht sailing

The sail of a yacht has the shape of airfoil

When a yacht sailing against the wind, its sail is rotated

On the windward side, it has a faster flow

On the leeward side, it has a slower flow

A force causing the yacht to move

Jets & Nozzles

When a fluid flow through a horizontal pipe from a large cross-section to a smaller cross-section, its velocity increases

The jets & nozzles are having a constriction to produce the effect

Example: Bunsen burner, Filter pump, Spray, Carburetors

Bunsen burner:

The town gas is injected to the Bunsen burner thou’ a jet

Faster flow & lower pressure

The lower pressure inside causes sucking of air from air hole

Higher oxygen-town gas ratio, better combustion

Filter pump:

When water passing thou’ the jet in filter pump, pressure dec.

The dec. in pressure sucks air from the chamber

The chamber is evacuated

Paint sprayer:

When air blown thou’ the nozzle, pressure at nozzle dec.

The dec. in pressure causes stagnant air inside exert pressure to push the paint out

Carburetor:

Carburetor is used to mix air w/fuel to prepare for the engine

When air is drawn thou’ the narrow duct, its pressure dec.

The reduced pressure sucks up fuel and mix w/air

The proportion of air & fuel is controlled by the pressure, i.e. size of duct

### Measuring devices:

Venturi meter:

Venturi meter is a horizontal pipe w/a constriction

Cross-sectional area of the pipe = A1; Fluid speed = v1

Cross-sectional area of the constriction = A2; Fluid speed = v2

Since A1v1 = A2v2 and,

Liquid level ( Pressure

Flow speed of fluid

Pitot Tube:

Pitot tube is a manometer w/two tubes, namely the total tube & static tube

At the mouth of total tube T, the fluid stagnates, fluid speed vt=0

At the mouth of static tube S, the fluid moves at speed vs = v

Flows at undisturbed flow speed

At points S & T, the pressures can be related by: or

Speed of flow:

## Gases

### Gas Law:

Boyle’s Law: For a fixed mass m of gas at constant temperature T, the pressure P of the gas is inversely proportional to its volume V

PV = Constant

Gases that obey Boyle’s law exactly is called ideal gas

Most gases obey Boyle’s law well at low pressure and high temperature

Pressure Law: At fixed m and V, P ( T

Charles’ Law: At fixed m and P, V ( T

Ideal gas equation: PV = n R T

R = Universal molar gas constant = 8.3145 J K–1mol–1

### Avogardro’s Law:

Under same V, T & P; two ideal gases contain equal number of molecules

In PaVa = naRTa	and  PbVb = nbRTb , if Pa=Pb; Va = Vb; Ta = Tb, then na = nb

1 mol ideal gas in std T (273.15K) & P (1.013(105 Pa) has a vol. 22.4 dm3

### Microscopic Definition of Ideal Gas:

Large separation btw molecules w.r.t. their size

Gas molecules occupy negligible volume

Gas molecules are point masses

Molecules are in random motion & obey Newton’s Laws

Molecules move in all directions with equal probability

Constant distribution of various molecular speeds

Gas molecules undergo perfectly elastic collision

Molecular kinetic energy is conserved

Intermolecular forces / interactions are short-range and negligible

Intermolecular attraction / repulsion would not alter the volume

### Kinetic Theory Model:

Assume a gas comprising N molecules each of mass m trapped in a cubic box of vol. (3

For a molecule moving with velocity , consider its x-direction component

When it collides with the wall of the cubic box, it undergoes perfectly elastic collision

The molecule rebounds in reversed direction with same speed

Momentum change p = mu – m(–u) = 2mu

After it rebounds, it moves toward the opposite wall

It collides with the wall on opposite side after time

Period for the molecule collides on the same wall:

Force exerted by the gas molecule over a long period:

Total force exerted by N molecules:

is the mean square speed of molecules

Pressure experienced by the wall:

Since ,  and

as gases are in random motion

By defining the root-mean-square speed

where n = no. of mole of gas; M = molar mass of gas

### Temperature & Energy:

( Pressure ( Molecular translational K.E. of the gas

Total internal energy of a gas:

Boltzmann’s constant == 1.3806 ( 10–23 JK–1

Avogardro’s number = NA = 6.022 ( 10–23 mol–1

(

Avg K.E. of gas molecule ( Absolute temperature of gas

### Distribution of molecular speeds:

and

R.m.s. Speed of gas molecule:

As the temperature inc., the rms speed of gas inc.

The various speed of gas follows the Maxwell-Boltzmann distribution

When temperature inc., the peak of the curve shift to right

Area under the curve = No. of molecules = Constant

Amplitude of curve falls as temperature inc.

The curve is spread out as temperature inc.

### Real Gases:

Real gases differ ideal gases as:

Have a finite size

Possess intermolecular interaction

Dipole-dipole interaction at most times

Electron cloud repulsion when collides

Due to the differences, the ideal gas equation PV = nRT is not applicable:

Pressure is less: When gas molecules strike on the wall, attraction retarded the effect

Volume is greater: Repulsive force reduces the space where a molecule can move

The gas molecules occupies spaces makes the measured volume  actual free volume

For pressure, a positive correction k is added

Pressure = P + k		where

Fore volume, a negative correction nb is made

Increase in volume ( Amount of gas molecules

Volume = V – nb

Van der Waals’ equation of state: 
			for some constants a and b w.r.t. to a particular gas

is the correction for the pressure affected by intermolecular attraction

nb is the correction for the volume affected by the volume occupied by molecular size

The van der Waals’ eqn accurately describing the behavior of real gas at high temperature

On or above the critical temperature

Above the critical temp., the P-V curve (isotherm) shows a rectangular hyperbola

At critical temp., the isotherm has a pt of inflexion C representing the critical point

At the critical point, gas, vapor & liquid exists in equilibrium

Below the critical temp., the isotherm has a part of flat curves

At the flat part of the curve, it is in liquid-vapor phase equilibrium

## Thermodynamics

Energy: The capacity to do work

Internal Energy: Total energy possessed by a substance or a system

Includes molecular kinetic energy and molecular potential energy

### Heat & Energy:

Matters possess internal energy due to its internal state

Molecular KE due to molecular motion

Measured by absolute temperature

Intermolecular PE due to intermolecular interactions

More separated molecules, greater PE

Internal energy U of an object may change by:

Work done W by the object

Heating the object to give it energy Q

By convection, conduction or radiation from one body to another

### Laws of Thermodynamics:

Zeroth law of thermodynamics states that when each of two systems is in equilibrium with a third, the first two systems must be in equilibrium with each other

First law of thermodynamics states that an object gains internal energy due to heat transfer and work done on it

U = Q – W

U = Change of internal energy

+	: Gain of internal energy
–	: Loss of internal energy

Q = Energy transferred during heating

+	: Energy transferred to the system
–	: Energy transferred out of the system

W = Work done

+	: Work done by the system on another
–	: Work done on the system by another

Second law of thermodynamics states that the entropy of an isolated system can never decrease

Heat-engine version: No continually working heat engine can take heat from a source and convert it completely into work

An isolated system is the one which U = Q = W = 0  (Internal energy keeps constant)

Maximum efficiency of a heat engine:

T2 = Source temperature in K

T1 = Sink temperature in K

Third law of thermodynamics states that the temperature of 0K can be approached arbitrarily closely, but it can never be reached

### Gas System:

A gas under pressure P and has a definite volume V, when it expands for V,
  Work done by the gas = PV =

When it expands, V  0, work done by the gas, W > 0, temperature dec.

When it compresses, V  0, work done on the gas, W < 0, temperature inc.

In isovolumetric process, keeping V = 0

W = 0, Q = U

In isobaric process, keeping P = 0

In isothermal process, keeping T = 0

The process is slow to allow heat exchange to maintain constant T

It is held in a thin-walled, highly conducting vessel surrounding by a constant temperature bath

As U ( T, U = 0

Q = W

In adiabatic process, Q = 0

No heat exchange occurred

The process is rapid to prevent heat exchange

It is held in a thick-walled, highly insulated vessel

U = –W

PV = constant		where

 = 1.67 for monoatomic gas;  = 1.40 for diatomic gas;  = 1.30 for polyatomic gas

### Degradation of energy:

The nature has a tendency to move toward a state of disorder

A higher grade energy can change to a lower grade energy completely;
a lower grade energy transform to a higher grade energy can never complete

Higher grade energy can be transformed w/higher efficiency

All the energy ultimately becomes internal energy of the surroundings thou’ being used to overcome friction, in which the internal energy is an useless energy

Energy is degraded

Primary energy resources: Naturally occurring fuels (e.g. coal, gas)

Secondary fuels: Electricity, petrol, etc.

Renewable sources: Energy sources that can be replenished naturally and thus inexhaustible

Example: Solar energy, wind, tidal, geothermal, wave

# Footnotes

Tensile stress is the stress to produce longitudinal elongation or compression

Streamlined flow = Steady flow

The critical temperature is the temperature above which a gas cannot be liquefied by applying high pressure

When gas above the critical temp., it is called as ‘gas’; when it is below the critical temp., it is called as ‘vapor’

Molecular motion cans be translational, rotational or vibrational motions

Work is a process to transfer energy from one body to another by means of application of a force for a distance

Heat is a process to transfer energy from one body to another by means of temperature difference